## Slide 1: MMA WBDDS HPDU Qualification Testing
454800-1007 Hydraulic Power Drive Unit
May 4 & 5, 2010

## Slide 2: Test Failures Resulting in Configuration Changes
Overview of significant failures which resulted in design changes in some of the major components shown below

## Slide 3
Summary of
Configuration Chronology by Failure Analysis Report (FAR) and dash number
FAR 001, Brake Impulse Test – Failure of Brake Cap Screws & mounting bolts (Upgrade to 454805-1003 Rev C)
  Upgrade Brake End Cap Bolts and Brake Mounting Bolts
FAR 002, 004 Load Profile Checkout – No-back Ring Fracture (-1005 Rev D & E)
  Increase No-back Ring thickness and change from 440C CRES material to 300M
  Replace No-back elastomer spring between rollers to a U-shaped sheet metal spring to reduce drag
FAR 014, Vibration Testing – Brake and Stop Module Failures (-1007 Rev F)
  Upgrade Brake Assy to 454894-1005 configuration with a new Cylinder Assy, End Disk, bolts and Slide
  Stop Module changes to use larger Anti-rotation Rods and End Cap bolts
  Replace many socket head cap screws with high strength 12-point bolts
  Add Thermal Spacer
  Add external drain for hydraulic motors
  Add Stop Module Bushing to prevent gears from coming out of mesh due to Stop Screw deflection
FAR 016, Motor Operated Endurance – Brake, Stop Module and No-back Spring failures (-1007 Rev G)
  Revised No-back to use shorter rollers, ½ length springs and Spring Keepers to prevent spring damage
  Increase grease to 1.5 pounds to allow gears pick up grease from bottom of gearbox and recirculate it
FAR 025, Motor Operated Endurance – Brake and Stop Module failures (-1007 Rev H)
  Upgrade Brake Assy to -1007 configuration with four Brake Disk Tabs to replace slotted disks and three posts
  Improve strength of Stop Screw
  Upgrade Stop Module Thrust Bearings with an increased capacity design
  Replace
  Add coil spring in Stop Module to provide thrust bearing preload to ensure rolling instead of slipping rollers
FAR 026, Motor Operated Endurance – Excessive Brake due to Stop Module Spring (-1007 Rev J)
  Remove coil spring due to excessive brake drag and heat
FAR 030, Motor Operated Endurance – No-back slipping after 3.2 lives (454800QSI015 → 454899-3 Spring Keeper)
FAR 031, Manual Drive Endurance – Skydrol contamination & fractured Brake Springs

## Slide 4: Pressure Impulse Testing Brake Cap mounting bolts
NAS1153 Flat Head Screws failed due to bending stresses under the head
High Strength MS21250 Bolts with large fillets under the head resolved Brake Cap and Mounting Bolt Failures
FAR 001

## Slide 5: Operation Under Load No-back Ring
440C CRES Ring fractured due to poor fracture toughness under hydraulic motor startup conditions at thin section (2% elongation)
FAR 002 & 004
Revised design with reduced ID to gain 50% increase in wall thickness and change to material to 300M for increased strength and ductility (8% elongation). Development test showed new design to be several times stronger than required

## Slide 6: Vibration Testing Brakes Assembly Upgrade
Bolts and posts failed due to motor stall loads and startup transient impact loads on posts
FAR 014
New Cylinder and high strength 3/8” bolts replace 3/16” bolts and stand-offs

## Slide 7: Vibration Testing Stop Module Upgrade
End Cap Screws loosened or broke due to rod twisting
FAR 014
Rod diameter increased, End Cap revised for increased compliance to reduce bolt bending stress in larger stronger bolts
Added Thermal Spacer to allow for thermal contraction of Aluminum Housings
Larger Thrust Bearing

## Slide 8: Vibration Testing Added External Motor Drain
High speed dynamic motor seal is designed to leak a small amount of hydraulic fluid (Skydrol) to maintain adequate lubrication (metal seal with surfaces lapped to a mirror finish).
Before the external drain was added, Skydrol was intended to drain at the bottom of the gearbox, instead the gears pick up the fluid and spay it with enough velocity to remove the grease.
FAR 014
Drain Block collects motor and brake leakage to an external drain bottle

## Slide 9: Motor Operated Endurance No-back Modification
Full length springs were damaged due to roller skewing
FAR 016
Added Spring Keeper:
prevents damage at ends to due to roller skewing
limits travel of rollers to protect springs from excessive deflection
keeps springs centered along roller
Springs were nested (not shown) to increase spring force

## Slide 10: Motor Operated Endurance Additional Brake Upgrade
As the HPDU drives out of an end stop at startup, the slotted disks allow the brake to rotate freely until the translating nut backs away from the brake to unload it.
FAR 025
Four Tabs per Disks replace three posts
Extensive dynamic analysis on impact of tabs into Cylinder legs was performed for each disk configuration
Endurance testing showed less Brinelling of tab surfaces than anticipated, indicating a conservative analysis
At motor startup, each slotted disk is accelerated from one end of the slot to the other. Due to a scaling error in test console data, the actual impact speed was much higher than the posts were designed to withstand.

## Slide 11: Motor Operated Endurance Additional Stop Module Upgrade
Final Apollo root cause activity indicates bearing damage due to overload as a result of the initial brake post failure. Brake failure results in a calculated 14,600 lb axial load in Stop Module and Brakes (57% overload).
FAR 025
To increase robustness in case of a brake failure, upgrades were made to the Stop Screw and Thrust Bearing
Single flat on each side of rollers with subsequent sliding and overheating
ISO 76 Static Load Rating: 6,830 lb (114% overload w/o mal-distribution, 180% with .005 screw runout and flexing of Bumper Stop
Improved runout tolerance on screw, better support and increased length rollers give a design solution meeting the ISO 76 load rating.

## Slide 12: Motor Operated Endurance - No-back Slipping
FAR 030
No-back slipped at Motor Start-up allowing motor to drive through the manual drive gearing instead of through the output shafts. No-back grabbed after a short period of time.
A few cycles later, the no-back slipped again and did not grab and testing was stopped.
13 out of 32 springs were found to be inactive, approx 40% reduction of spring force

## Slide 13: Manual Drive Endurance Skydrol Contamination & Fractured Springs
FAR 031
Motor evaluation at HSD revealed a static seal that normally rotates with the shaft was slipping and wearing
Static seal leakage bypassed the dynamic seal
Corrective action was simply to increase surface roughness of the shaft interface

## Slide 14: Manual Drive Endurance Skydrol Contamination
FAR 031
Skydrol replaced grease film layer, increasing the coefficient of friction of the no-back
Torque to drive the door open under simulated door preload increased above MDA slip clutch setting
No-back operated normally under low loads and resisting loads .

## Slide 15: Manual Drive Endurance Fractured Brake Springs
FAR 031
For System A & B brakes, 61 out of 192 (32%) springs broken
1075 Steel at 49 Rc hardness
LS-DYNA model simulated 5 cycles to flat height and then cycled to installed and compressed height predicted 20,000 cycle life.
Failed at less than 24,000 cycles

## Slide 16: Manual Drive Endurance Brake Spring Corrective Action
FAR 031
302 CRES spring of same design (alternate: 1075 spring more tightly controlled)
LS-DYNA model correctly predicts location of initial fracture at ID corner
There are 2 spring cycles per door cycle: 2(4950) = 9,900 cycles (design to 8 lives = 8(9,900) = 79,200 cycles)
Element 2149
Element 2122
(at corner)
t = 1 s